WMF-C Series

SMD Type NTC Thermistors贴片型负温度系数热敏电阻器

- For Temperature Compensation & Sensing

用于温度补偿和温度探测

■ GENERAL 概述

1. Features

* Highly reliable multilayer and monolithic structure , Leadless, ideal for high density SMT installation。

* Superior heat resistance to reflow or wave soldering and excellent solderability thanks to three metallic layers。

* Low floating Capacitance(less 3pF),Can be use (using TCXO) in the high frequency region, Fast Response。

* Excellent Heat Dissipation Constant and Temperature Coefficient, Wide ranges of operating temperature(-40 to 125℃)。

2. Recommended Applications

Equipment related to mobile communication TCXOs (temperature compensated type quartz oscillator), RF circuits(power amp circuits, temperature monitoring circuits) LCD panel. Temperature compensated crystal oscillator, which is the key device for mobile phones.

* Temperature compensating circuit of LCD.

* Temperature sensing in rechargeable batteries and chargers.

* Temperature sensor for CPU.

* IC and Semiconductor protecting.IC

* Printer temperature compensating circuit.

* Player Driver.

* Telecom exchanger .

* DC/AC transformer and HIC over heat protecting.

* Temperature compensation in a variety of other circuits

1. 特性

* 高可靠的叠层片式陶瓷结构体积小，无引线，适合高

强度表面贴装。

* 端电极采用三层电镀具有良好的可焊性及耐热冲击

性，适合波峰焊及再流焊。

* 分布容量低，可应用于高频领域，响应速度快。

* 优良的耗散系数和温度系数，工作温度范围广：-40~

+125℃

2. 应用领域

移动通信中使用的温补石英晶荡器（TCXO）射频电

路(临界温度监视），LCD面板。

* 液晶显示器温度补偿电路

* 可充电电池及充电器的温度探测

* 计算机微处理器的温度探测

* 和半导体器件过热保护

* 打印头温补

* 播放机驱动器

* 有线通信程控交换机

* DC/AC转换器和HIC的过热保护

* 需温度补偿的各种电路

■ PART NUMBERING 产品编号

| WMFC | - | 0603 | R103 | J | B3435 | F | B | R |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |

⑴        ⑵     ⑶    ⑷     ⑸     ⑹   ⑺   ⑻

⑴ Series系列：WMFC 详见右图和下表，See right-hand chart and table below

⑵ Sizes尺寸： 0402 – 1.0×0.5×0.5  0603 - 1.6×0.8×0.6   0805 – 2.0×1.2×0.6

⑶ Rated Zero Power Resistance额定零功率电阻值103-10×103Ω

⑷ R25 Tolerance R25误差 F-±1% G-±2% H-±3% J-±5% K-±10%

| ⑸ B value B值:B3435- B=3435K Code | L1 | W | H | L2 |
| --- | --- | --- | --- | --- |
| 0402 | 1.0±0.15 | 0.5±0.15 | 0.5±0.15 | 0.5±0.20 |
| 0603 | 1.6±0.20 | 0.8±0.20 | 0.6±0.20 | 1.0±0.20 |
| 0805 | 2.0±0.20 | 1.2±0.20 | 0.6±0.20 | 1.0±0.20 |

⑹ B值误差F-±1% H-±3%

⑺ Packing Type 包装形式：Ｒ－Reel盘装  Ｂ－Bulk散装

⑻ Special Code (RoHS) 特别代码：

R-Compliance with RoHS ( e.g. Pb Free ) 符合RoHS要求 ( 如: 不含铅 )

1.

■ SPECIFICATION S TABLE规格表

| No. 序号 | Part No. 产品编号 | Rated Zero Power Resistance 额定零功率电阻 R25 (KΩ) | B Value B值 （K） | Thermal Dissipation Constant 热耗散系数 δ(mW/℃) | Rated power 额定功率 P（mw） |  | Thermal Time Constant 热时间常数 τ(Sec) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | WMF-C-0402R101□B2700 | 0.1 | 2,700 | 1.0 | 100 |  | ≤3 |
| 2 | WMF-C-0402R221□B2750 | 0.22 | 2,750 |  |  |  |  |
| 3 | WMF-C-0402R331□B2800 | 0.33 | 2,800 |  |  |  |  |
| 4 | WMF-C-0402R471□B2850 | 0.47 | 2,850 |  |  |  |  |
| 5 | WMF-C-0402R681□B2900 | 0.68 | 2,900 |  |  |  |  |
| 6 | WMF-C-0402R102□B3000 | 1.0 | 3,000 |  |  |  |  |
| 7 | WMF-C-0402R222□B3100 | 2.2 | 3,100 |  |  |  |  |
| 8 | WMF-C-0402R222□B3900 | 2.2 | 3,900 |  |  |  |  |
| 9 | WMF-C-0402R332□B3200 | 3.3 | 3,200 |  |  |  |  |
| 10 | WMF-C-0402R472□B3250 | 4.7 | 3,250 |  |  |  |  |
| 11 | WMF-C-0402R682□B3350 | 6.8 | 3,350 |  |  |  |  |
| 12 | WMF-C-0402R103□B3435 | 10 | 3,435 |  |  |  |  |
| 13 | WMF-C-0402R103□B3900 | 10 | 3,900 |  |  |  |  |
| 14 | WMF-C-0402R153□B3500 | 15 | 3,500 |  |  |  |  |
| 15 | WMF-C-0402R223□B3800 | 22 | 3,800 |  |  |  |  |
| 16 | WMF-C-0402R333□B3900 | 33 | 3,900 |  |  |  |  |
| 17 | WMF-C-0402R473□B3900 | 47 | 3,900 |  |  |  |  |
| 18 | WMF-C-0402R473□B4050 | 47 | 4,050 |  |  |  |  |
| 19 | WMF-C-0402R683□B3950 | 68 | 3,950 |  |  |  |  |
| 20 | WMF-C-0402R104□B4100 | 100 | 4,100 |  |  |  |  |
| 21 | WMF-C-0402R154□B4050 | 150 | 4,050 |  |  |  |  |
| 22 | WMF-C-0402R224□B4050 | 220 | 4,050 |  |  |  |  |
| 23 | WMF-C-0402R334□B4100 | 330 | 4,100 |  |  |  |  |
| 24 | WMF-C-0402R474□B4150 | 470 | 4,150 |  |  |  |  |
| 25 | WMF-C-0402R564□B4200 | 560 | 4,200 |  |  |  |  |
| 26 | WMF-C-0402R105□B4500 | 1000 | 4,500 |  |  |  |  |
| 27 | WMF-C-0603R101□B2700 | 0.1 | 2,700 | 2.0 |  | 200 | ≤5 |
| 28 | WMF-C-0603R221□B2750 | 0.22 | 2,750 |  |  |  |  |
| 29 | WMF-C-0603R331□B2800 | 0.33 | 2,800 |  |  |  |  |
| 30 | WMF-C-0603R471□B2850 | 0.47 | 2,850 |  |  |  |  |
| 31 | WMF-C-0603R681□B2900 | 0.68 | 2,900 |  |  |  |  |
| 32 | WMF-C-0603R102□B3000 | 1.0 | 3,000 |  |  |  |  |
| 33 | WMF-C-0603R222□B3100 | 2.2 | 3,100 |  |  |  |  |
| 34 | WMF-C-0603R222□B3900 | 2.2 | 3,900 |  |  |  |  |
| 35 | WMF-C-0603R332□B3200 | 3.3 | 3,200 |  |  |  |  |
| 36 | WMF-C-0603R472□B3250 | 4.7 | 3,250 |  |  |  |  |
| 37 | WMF-C-0603R682□B3350 | 6.8 | 3,350 |  |  |  |  |
| 38 | WMF-C-0603R103□B3435 | 10 | 3,435 |  |  |  |  |
| 39 | WMF-C-0603R103□B3600 | 10 | 3,600 |  |  |  |  |
| 40 | WMF-C-0603R103□B3900 | 10 | 3,900 |  |  |  |  |
| 41 | WMF-C-0603R153□B3600 | 15 | 3,600 |  |  |  |  |
| 42 | WMF-C-0603R223□B3900 | 22 | 3,900 |  |  |  |  |
| 43 | WMF-C-0603R333□B4000 | 33 | 4,000 |  |  |  |  |
| 44 | WMF-C-0603R473□B3900 | 47 | 3,900 |  |  |  |  |
| 45 | WMF-C-0603R473□B4150 | 47 | 4,150 |  |  |  |  |
| 46 | WMF-C-0603R683□B4050 | 68 | 4,050 |  |  |  |  |
| 47 | WMF-C-0603R104□B4000 | 100 | 4,000 |  |  |  |  |

| No. 序号 | Part No. 产品编号 | Rated Zero Power Resistance 额定零功率电阻 R25 (KΩ) | B Value B值 （K） | Thermal Dissipation Constant 热耗散系数 δ(mW/℃) | Rated power 额定功率 P（mw） |  |  | Thermal Time Constant 热时间常数 τ(Sec) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 48 | WMF-C-0603R104□B4250 | 100 | 4,250 | 2.0 |  | 200 |  | ≤5 |
| 49 | WMF-C-0603R154□B4050 | 150 | 4,050 |  |  |  |  |  |
| 50 | WMF-C-0603R224□B4100 | 220 | 4,100 |  |  |  |  |  |
| 51 | WMF-C-0603R334□B4100 | 330 | 4,100 |  |  |  |  |  |
| 52 | WMF-C-0603R474□B4200 | 470 | 4,200 |  |  |  |  |  |
| 53 | WMF-C-0603R564□B4200 | 560 | 4,200 |  |  |  |  |  |
| 54 | WMF-C-0603R105□B4500 | 1000 | 4,500 |  |  |  |  |  |
| 55 | WMF-C-0805R101□B2700 | 0.1 | 2,700 | 3.0 | 300 |  | ≤10 |  |
| 56 | WMF-C-0805R221□B2750 | 0.22 | 2,750 |  |  |  |  |  |
| 57 | WMF-C-0805R331□B2800 | 0.33 | 2,800 |  |  |  |  |  |
| 58 | WMF-C-0805R471□B2850 | 0.47 | 2,850 |  |  |  |  |  |
| 59 | WMF-C-0805R681□B2900 | 0.68 | 2,900 |  |  |  |  |  |
| 60 | WMF-C-0805R102□B3000 | 1.0 | 3,000 |  |  |  |  |  |
| 61 | WMF-C-0805R222□B3100 | 2.2 | 3,100 |  |  |  |  |  |
| 62 | WMF-C-0805R222□B3900 | 2.2 | 3,900 |  |  |  |  |  |
| 63 | WMF-C-0805R332□B3200 | 3.3 | 3,200 |  |  |  |  |  |
| 64 | WMF-C-0805R472□B3250 | 4.7 | 3,250 |  |  |  |  |  |
| 65 | WMF-C-0805R682□B3350 | 6.8 | 3,350 |  |  |  |  |  |
| 66 | WMF-C-0805R103□B3435 | 10 | 3,435 |  |  |  |  |  |
| 67 | WMF-C-0805R103□B3600 | 10 | 3,600 |  |  |  |  |  |
| 68 | WMF-C-0805R103□B3900 | 10 | 3,900 |  |  |  |  |  |
| 69 | WMF-C-0805R153□B3600 | 15 | 3,600 |  |  |  |  |  |
| 70 | WMF-C-0805R223□B3900 | 22 | 3,900 |  |  |  |  |  |
| 71 | WMF-C-0805R333□B4000 | 33 | 4,000 |  |  |  |  |  |
| 72 | WMF-C-0805R473□B3900 | 47 | 3,900 |  |  |  |  |  |
| 73 | WMF-C-0805R473□B4150 | 47 | 4,150 |  |  |  |  |  |
| 74 | WMF-C-0805R683□B4150 | 68 | 4,150 |  |  |  |  |  |
| 75 | WMF-C-0805R104□B4100 | 100 | 4,100 |  |  |  |  |  |
| 76 | WMF-C-0805R104□B4300 | 100 | 4,300 |  |  |  |  |  |
| 77 | WMF-C-0805R224□B4200 | 220 | 4,200 |  |  |  |  |  |
| 78 | WMF-C-0805R334□B4200 | 330 | 4,200 |  |  |  |  |  |
| 79 | WMF-C-0805R474□B4200 | 470 | 4,200 |  |  |  |  |  |
| 80 | WMF-C-0805R564□B4300 | 560 | 4,300 |  |  |  |  |  |
| 81 | WMF-C-0805R105□B4500 | 1,000 | 4,500 |  |  |  |  |  |

可根据客户订做阻值规格，□阻阻精度可选。