WMZ91/ 92/ 93 Series

PTC Thermistors正温度系数热敏电阻器

- For Starting Protection of Inventor & Compressors

用于变频器、压缩机启动保护

■ GENERAL 概述

- PTC thermistors for starting refrigerator compressor:

Refrigerator compressor is driven by single-phase induction motor. The start-up of motor needs to overcome the inertia of itself, and also the load—the back-action strength of high-pressure refrigeration agent, which requires high start-up current and torque. When the motor is operating normally, the torque required will decrease substantially. Therefore, usually the following start-up circuit (Figure 1) is adopted to establish PTC thermistors in series in start-up coil. When the motor is connected with power, PTC is in low resistance, and the motor is started under the joint functioning of start-up coil and operating coil, and after 0.4-3s, the resistance of PTC will increase by several orders of magnitude because of its own heat, which is equivalent to cutting off start-up coil to enable normal operation of major coil, so that the starting process is accomplished.

2. PTC thermistors for starting frequency conversion air-conditioner

When starting frequency conversion air-conditioner, the voltage is added to the whole wave filtration circuit through PTC components to recharge the capacitor stably to the preset value, and the power module IPM begins to work and transform inversely the input DC voltage into 3 lines of AC power added on the coils of 3-phase motor, to enable the normal operation of motor. In the mean time, after the capacitor is recharged to the preset value, the IPM will output DC low voltage to the relay pick-up switch to short-circuit and stop the PTC components. (Figure 2)

The function of series PTC components in main loop is to avoid the impact of high current on rectification wave-filtration circuit and consequently the damage of energy-conservation components during the initial period of galvanization. That is, PTC components function as a buffer and protector. Besides, in case of the failure (unable to pick up normally) of relay, PTC components will have high resistance, which can protect the circuit.

1. 冰箱、饮水机、制冰机压缩机启动用PTC热敏电阻器

制冷压缩机由单相感应电机驱动。启动时，压缩机既要克服本身的惯性，又要克服负载——高压制冷剂的反作用力，因而需要提供较大转矩及驱动电流; 启动后, 压缩机处于正常运转状态，需要的转矩及驱动电流将大幅度下降。制冷压缩机典型启动电路如图1.所示: 通常将PTC热敏电阻器串联于启动绕组。开始通电时，PTC处于低阻态，电机在启动绕组和运行绕组的共同作用下启动，经过0.2~3S后，PTC因自热导致电阻值快速跃升若干数量级，从而使启动绕组切断,令主绕组进入正常运转状态。

2. 变频空调启动用PTC热敏电阻器

如图2.所示:变频空调启动时，电压经过PTC元件加到整个滤波电路上，对电容器平稳充电至设定值，功率模块IPM开始工作，将输入的直流电压逆变为三只交流电加到三相电机绕组上，使电机正常运转。同时电容器充电至设定值后，经IPM输出一直流低电压至继电器吸合开关K，PTC元件被短接，停止工作。

主回路中串接PTC元件的作用是：避免在通电初期，整流滤波电路直接承受大电流的冲击，造成储能元件受损。即PTC元件在通电初期起一个缓冲与保护的作用。此外，若继电器失效（无法正常吸合）时，PTC元件成为高阻态，可对电路进行保护。

■ PART NUMBERING 产品编号

| WMZ91 | - | 120 | HL | 33R | M | 355 |
| --- | --- | --- | --- | --- | --- | --- |

⑴        ⑵     ⑶    ⑷     ⑸     ⑹

⑴ Series系列：WMZ91 – Chip Type 芯片型  	WMZ92 - Encased Type 壳装型 	WMZ93- Coating Type 焊接包封型

⑵ Curie Temperature居里温度105-105+10-5℃  120-120±7℃  135-135±7℃

⑶ Dimension尺寸 HL-Ø16.0*2.5mm  JL-Ø17.0*2.5mm  LL-Ø 19.5*2.5mm  LM-Ø19.5*3.2mm  LN-Ø19.5*5.0mm

⑷ Rated Zero Power Resistance额定零功率电阻R：33R - 33Ω　4R7 –4.7Ω  101-100Ω

⑸ Tolerance of Resistance阻值允差：M - ±20%  V - ±25%　X - +30% / - 20%

⑹ WMZ91/92系列：Max. Operating Vol. 最大工作电压: 180V  250V  300V  355V  450V

WMZ92B系列：Rate Operating Vol. 额定工作电压: 110-110V  220-220V

WMZ91型                              WMZ92型                               WMZ93型

■ SPECIFICATION S TABLE规格表

☆WMZ91

| No. 序号 | Part No. 产品编号 | Rated Zero Power Resistance 额定零功率 电阻 RN (Ω) | Curie Temperature 居里温度 Tc (℃) | Maximum voltage 最大电压 Umax (V) | Maximum current 最大电流Imax (A) | Start-up time 启动时间 t0 (S) | Power consumption 消耗功率 Pmax (W) | Restoration time 恢复时间 trmax (S) | Coil resistance 线圈电阻Rref (Ω) | Dimension 尺 寸 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  | Diameter 直径 D (mm) | Thickness 厚度 T (mm) |
| 1 | WMZ91-105HL5R0M180 | 5.0 | 105+10-5 | 180 | 12 | 0.2-1.2 | 3.0 | 110 | 10 | 16.0±0.5 | 2.5±0.2 |
| 2 | WMZ91- 105HL6R8M180 | 6.8 |  | 180 | 12 | 0.2-1.2 | 3.0 | 105 | 10 |  |  |
| 3 | WMZ91-105HL10RM180 | 10 |  | 180 | 12 | 0.2-1.2 | 3.0 | 95 | 10 |  |  |
| 4 | WMZ91- 105HL22RM300 | 22 |  | 350 | 7 | 0.2-1.2 | 3.0 | 105 | 25 |  |  |
| 5 | WMZ91-105HL33RM355 | 33 |  | 355 | 6 | 0.2-1.2 | 3.0 | 110 | 25 |  |  |
| 6 | WMZ91-120HL4R7M180 | 4.7 | 120±7 | 180 | 12 | 0.2-1.3 | 3.3 | 85 | 10 | 16.0±0.5 | 2.5±0.2 |
| 7 | WMZ91-120HL6R8M200 | 6.8 |  | 180 | 10 | 0.2-1.2 | 3.3 | 90 | 10 |  |  |
| 8 | WMZ91-120HL15RM350 | 15 |  | 350 | 8 | 0.2-1.2 | 2.8 | 100 | 30 |  |  |
| 9 | WMZ91-120HL22RM350 | 22 |  | 350 | 7 | 0.2-1.0 | 2.8 | 85 | 30 |  |  |
| 10 | WMZ91-120HL33RM355 | 33 |  | 355 | 6 | 0.2-1.0 | 2.8 | 90 | 55 |  |  |
| 11 | WMZ91-120HL47RM350 | 47 |  | 350 | 5 | 0.2-1.0 | 2.8 | 80 | 30 |  |  |
| 12 | WMZ91-135HL3R3M160 | 3.3 | 135±7 | 160 | 12 | 0.4-1.3 | 3.5 | 90 | 25 | 16.0±0.5 | 2.5±0.2 |
| 13 | WMZ91-135HL4R7M180 | 4.7 |  | 180 | 12 | 0.4-2.5 | 3.5 | 85 | 10 |  |  |
| 14 | WMZ91-135HL6R8M200 | 6.8 |  | 200 | 10 | 0.2-1.5 | 3.0 | 75 | 10 |  |  |
| 15 | WMZ91-135HL10RM200 | 10 |  | 200 | 8 | 0.2-1.5 | 3.0 | 65 | 25 |  |  |
| 16 | WMZ91-135HL15RM350 | 15 |  | 350 | 8 | 0.15-1.0 | 2.8 | 60 | 30 |  |  |
| 17 | WMZ91-135HL22RM350 | 22 |  | 300 | 7 | 0.2-1.0 | 2.8 | 65 | 30 |  |  |
| 18 | WMZ91-135HL33RM355 | 33 |  | 355 | 6 | 0.2-1.0 | 2.8 | 60 | 55 |  |  |
| 19 | WMZ91-135HL47RM400 | 47 |  | 400 | 5 | 0.2-1.0 | 3.5 | 60 | 25 |  |  |
| 20 | WMZ91-135HL68RM400 | 68 |  | 400 | 4 | 0.2-1.0 | 3.5 | 60 | 55 |  |  |

| No. 序号 | Part No. 产品编号 | Rated Zero Power Resistance 额定零功率 电阻 RN (Ω) | Curie Temperature 居里温度 Tc (℃) | Maximum voltage 最大电压 Umax (V) | Maximum current 最大电流Imax (A) | Start-up time 启动时间 t0 (S) | Power consumption 消耗功率 Pmax (W) | Restoration time 恢复时间 trmax (S) | Coil resistance 线圈电阻Rref (Ω) | Dimension 尺 寸 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  | Diameter 直径 D (mm) | Thickness 厚度 T (mm) |
| 21 | WMZ91-120JL4R7M180 | 4.7 | 120±7 | 180 | 12 | 0.3-1.5 | 3.5 | 100 | 10 | 17.0±0.5 | 2.5±0.2 |
| 22 | WMZ91-120JL5R5M200 | 5.5 |  | 200 | 10 | 0.3-1.5 | 3.5 | 90 | 10 |  |  |
| 23 | WMZ91-120JL10RM200 | 10 |  | 200 | 10 | 0.2-1.5 | 3.5 | 90 | 10 |  |  |
| 24 | WMZ91-120JL20RM300 | 20 |  | 300 | 8 | 0.2-1.3 | 3.5 | 85 | 30 |  |  |
| 25 | WMZ91-120JL33RM355 | 33 |  | 355 | 6 | 0.2-1.3 | 3.5 | 85 | 55 |  |  |
| 26 | WMZ91-120LL4R7M180 | 4.7 | 120±7 | 180 | 12 | 0.5-2.5 | 3.5 | 100 | 10 | 19.5±1.0 | 2.5±0.2 |
| 27 | WMZ91-120LL6R8M200 | 6.8 |  | 200 | 10 | 0.2-1.5 | 3.5 | 100 | 25 |  |  |
| 28 | WMZ91-120LL15RM350 | 15 |  | 350 | 8 | 0.2-1.5 | 3.0 | 100 | 30 |  |  |
| 29 | WMZ91-120LL22RM350 | 22 |  | 350 | 7 | 0.2-1.5 | 3.0 | 85 | 30 |  |  |
| 30 | WMZ91-120LL33RM355 | 33 |  | 355 | 6 | 0.2-1.5 | 3.0 | 85 | 55 |  |  |
| 31 | WMZ91-120LL47RM400 | 47 |  | 400 | 5 | 0.2-1.5 | 3.0 | 75 | 55 |  |  |
| 32 | WMZ91-135LL4R7M180 | 4.7 | 135±7 | 180 | 12 | 0.5-2.5 | 3.5 | 90 | 10 | 19.5±1.0 | 2.5±0.2 |
| 33 | WMZ91-135LL6R8M200 | 6.8 |  | 200 | 10 | 0.2-1.5 | 3.5 | 90 | 15 |  |  |
| 34 | WMZ91-135LL15RM350 | 15 |  | 350 | 8 | 0.2-1.5 | 3.5 | 100 | 30 |  |  |
| 35 | WMZ91-135LL22RM350 | 22 |  | 350 | 7 | 0.2-1.5 | 3.5 | 80 | 30 |  |  |
| 36 | WMZ91-135LL33RM355 | 33 |  | 355 | 6 | 0.2-1.5 | 3.3 | 65 | 55 |  |  |
| 37 | WMZ91-135LL47RM400 | 47 |  | 400 | 5 | 0.2-1.5 | 3.0 | 60 | 55 |  |  |
| 38 | WMZ91-120LM4R7M180 | 4.7 | 120±7 | 180 | 12 | 0.2-2.5 | 4.0 | 120 | 25 | 19.5±1.0 | 3.2±0.2 |
| 39 | WMZ91-120LM6R8M200 | 6.8 |  | 200 | 10 | 0.2-2.0 | 4.0 | 120 | 10 |  |  |
| 40 | WMZ91-120LM10RM250 | 10 |  | 250 | 10 | 0.2-2.0 | 4.0 | 110 | 15 |  |  |
| 41 | WMZ91-120LM15RM350 | 15 |  | 250 | 8 | 0.2-1.5 | 3.5 | 100 | 30 |  |  |
| 42 | WMZ91-120LM30RM350 | 30 |  | 350 | 6 | 0.2-1.5 | 3.5 | 100 | 30 |  |  |
| 43 | WMZ91-120LM40RM350 | 40 |  | 350 | 5 | 0.2-1.5 | 3.5 | 100 | 30 |  |  |
| 44 | WMZ91-120LN15RM250 | 15 | 120±7 | 250 | 8 | 0.5-5.0 | 5.0 | 130 | 25 | 19.5±1.0 | 5.0±0.2 |
| 45 | WMZ91-120LN25RM300 | 25 |  | 300 | 7 | 0.5-5.0 | 5.0 | 120 | 25 |  |  |
| 46 | WMZ91-120LN30RM350 | 30 |  | 350 | 6 | 0.5-4.0 | 4.0 | 120 | 25 |  |  |
| 47 | WMZ91-120LN40RM350 | 40 |  | 350 | 5 | 0.5-4.0 | 4.0 | 110 | 25 |  |  |

☆WMZ92

| No. 序号 | Part No. 产品编号 | Rated Zero Power Resistance 额定零功率电阻 RN (Ω) | Curie Temperature 居里温度 Tc (℃) | Maximum voltage 最大电压 Umax (V) | Maximum current 最大电流Imax (A) | Start-up time 启动时间 t0 (S) | Power consumption 消耗功率 Pmax (W) | Restoration time 恢复时间 trmax (S) | Coil resistance 线圈电阻Rref (Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | ###### WMZ92-4R7M180 | 4.7 | 120±7 | 180 | 12 | 0.2-2.5 | 4.0 | 120 | 10 |
| 2 | WMZ92-6R8M200 | 6.8 |  | 200 | 10 | 0.2-2.5 | 4.0 | 120 | 10 |
| 3 | WMZ92-15RM350 | 15 |  | 350 | 8 | 0.2-1.5 | 3.5 | 110 | 30 |
| 4 | WMZ92-22RM350 | 22 |  | 350 | 7 | 0.2-1.5 | 3.5 | 105 | 30 |
| 5 | WMZ92-33RM350 | 33 |  | 350 | 6 | 0.2-1.5 | 3.3 | 95 | 30 |
| 6 | WMZ92-40RM350 | 40 |  | 350 | 5 | 0.2-1.5 | 3.3 | 95 | 30 |
| 7 | WMZ92-47RM350 | 47 |  | 350 | 5 | 0.2-1.2 | 3.3 | 85 | 30 |
| 8 | WMZ92-68RM350 | 68 |  | 350 | 4 | 0.2-1.2 | 3.3 | 80 | 30 |
| 9 | WMZ92-101RM350 | 100 |  | 350 | 3.5 | 0.1-1.0 | 3.3 | 80 | 30 |

☆WMZ93

| No. 序号 | Part No. 产品编号 | Rated Zero Power Resistance 额定零功率电阻 RN (Ω) | Curie Temperature 居里温度 Tc (℃) | Maximum voltage 最大电压 Umax (V) | Maximum current 最大电流Imax (A) | Start-up time 启动时间 t0 (S) | Power consumption 消耗功率 Pmax (W) | Restoration time 恢复时间 trmax (S) | Coil resistance 线圈电阻Rref (Ω) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | ###### WMZ93-125HL15RM200 | 15±20% | 120±7 | 110 | 8 | 0.2-1.5 | 4.5 | 120 | 10 |
| 2 | WMZ93-125HL22RM350 | 22±20% | 120±7 | 220 | 7 | 0.2-1.5 | 4.5 | 110 | 30 |
| 3 | WMZ93-125HL33RM350 | 33±20% | 120±7 | 220 | 6 | 0.2-1.5 | 4.5 | 105 | 30 |
| 4 | WMZ93-125HL40RM350 | 40±20% | 120±7 | 220 | 5 | 0.2-1.5 | 4.0 | 95 | 30 |
| 5 | WMZ93-125HL47RM350 | 47±20% | 120±7 | 220 | 5 | 0.2-1.5 | 4.0 | 95 | 30 |
| 6 | WMZ93-125HL60RM350 | 60±20% | 120±7 | 220 | 4 | 0.2-1.2 | 4.0 | 85 | 30 |
| 7 | WMZ93-125HL68RM350 | 68±20% | 120±7 | 220 | 4 | 0.2-1.2 | 4.0 | 80 | 30 |
| 8 | WMZ93-125HL101RM350 | 100±20% | 120±7 | 220 | 3.5 | 0.2-1.0 | 4.0 | 80 | 30 |